DURASTIC LIGHTWEIGHT UNDERLAY

DURASTIC LIGHTWEIGHT UNDERLAY has been developed as an exceptionally light, one coat, seamless, synthetic latex based underlay for use under vinyl tiles, vinyl sheets, linoleum, carpet, epoxy flooring etc.

WHERE LAID

Throughout the interior of all types of ships (including wet spaces) as an underlay for all types of approved decorative and functional coverings (i.e. tile and sheet vinyl, linoleum, tile and sheet rubber, carpet, ceramic tiles, epoxy coatings, and polyurethane finishes etc.)

TECHNICAL DATA

DENSITY:

900 kg per m3.

THICKNESS:

5-15 mm per coat.

LAID WEIGHT:

0.90 kg per m²  per mm thickness.

COMPRESSIVE STRENGTH:

To BS. 6319 Part 2 :1983  Is  6 N/mm².

FLEXURAL STRENGTH:

To BS. 6319 Part 3 : 1990  2.7 N/mm² with a displacement of 3.1mm.

BOND STRENGTH:

Adhesion tested and accepted as being within requirements laid down by the Department of Transport  (Marine Directorate) Survey of Crew Accommodation Merchant Ships - Instructions for the Guidance of Surveyors.

To BS 6319 (Slant Shear Method) Part 4 : 1984 is 4 N/mm²

THERMAL CONDUCTIVITY:

0.4 W/m K.

SURFACE PREPARATION

STEEL

Steel deck plates must be free from oil, grease, dirt, rust, loose paint etc.

It is essential that all traces of grease and oil are removed before application of the underlay.

A proprietary degreaser should be used.  The steel should be mechanically wire brushed to remove dirt, rust etc., paying particular attention along plate welds and boundary edges.

A mechanical discing machine using 7 inch No. 16 grit (Coarse) discs can be used on heavier deposits.

On older steel in poor condition with a heavier build up of old paint and, perhaps, pitted areas of corrosion it may be necessary to shot blast.

In all cases once the steel has been cleaned and roughened the underlay should be applied as soon as possible before any further rust develops.

ALUMINIUM

Aluminium deck plates must be free from oil, grease, dirt, loose paint etc.

It is essential that all traces of grease and oil are removed before application of the underlay.

A proprietary degreaser should be used.

After degreasing, a coat of Durastic CR60 should be applied and allowed to dry for a minimum of 8 hours, before application of the Durastic underlay.

SHOP PRIMERS

Because of the diversity of shop primers for steel it is impossible to give compatibility information for our underlays with each specific primer in this short section.

However we can say that Durastic Underlays can be applied over a wide range of primers.  In particular the popular rapid curing thin coat two-pack primers are suitable.

Primers containing zinc pigments such as silicates or phosphates usually have tie coats applied to prevent salt formation which makes them suitable.

Normally on a “new build” by the time the deck is released for underlay application the primer is almost walked off.  The installer should have checked that tie-coats had been applied if necessary and then the deck should be prepared by degreasing and removing dirt etc. with a wire brush as detailed in the steel preparation section.

We must stress that if there are any doubts about the type of paint we would much prefer that the installer tell us what primer is on the deck and we will establish with the paint manufacturer the type of paint system before deciding on its compatibility.

COVERAGE

- Lightweight Powder 		3 Bags  56kg

- Lightweight Liquid		1 Drum 25Kg

- covers 8 m² at 10mm

MIXING

For small areas, mixing can be carried out in a steel tray, or a cut down steel drum, using a garden hoe.  For larger areas, a ½ bag cement mixer is ideal.

The appropriate amount of Lightweight Liquid should be poured into the mixer and the Lightweight Powder gradually added, and well mixed until a workable consistency is obtained.  Do not overmix.  The Lightweight Liquid should always be placed into the mixing vessel first.

Note: Owing to varying climatic conditions, it may be found necessary to adjust the quantity of powder to attain the most suitable working consistency.

APPLICATION

The underlay should be spread on the clean deck plates, using a steel trowel to level off to the required thickness.  The underlay should not be overtrowelled.

Ambient temperatures should not be below 10°C on application.

PACKAGING

POWDER	Net:	18.6 kg

Gross:	18.8 kg

LIQUID	Net:	25.0 kg

Gross:	26.0 kg

STORAGE AND SHELF-LIFE

LIghtweight powder must be kept in a dry store.  Lightweight liquid must not be subjected to temperatures below  5°C or above 30°C.  Both materials can be stored for a period of 12 months when the above storage conditions prevail.

CERTIFICATES AND APPROVALS

Durastic Lightweight Underlay has been tested and approved as a primary underlay fulfilling the requirements of IMO Resolution A.653(16) and A.687(17) and the International Code for Application of Fire Test Procedures Annex 1 Part 2.

Durastic Lightweight  Underlay complies with the Marine Equipment Directive and has been approved by the leading Marine Approval Societies.  These approvals are updated on an ongoing basis and copies of certificates are available on request.

All materials are manufactured and tested using our Quality Management System which has been approved by Lloyds Register Quality Assurance Limited to 1S0 9001 : 2008.

HEALTH AND SAFETY

Normal precautions to avoid inhaling the dust when mixing the powder and to avoid getting the wet product on the skin (as cements are alkaline) should be observed.

Detailed Material Safety Data Sheets and C.O.S.H.H. Assessments are available for safe working with the product.  These should be consulted before commencing work to ensure safe working practice.

TECHNICAL ADVICE

This Data Sheet, although comprehensive, cannot cover every possible application.  Our Technical Department +44 (0) 191 483 2299 will be pleased to advise on specific applications.

IF IN DOUBT - ASK!