DURASTIC ACCODEK OUTSIDE DECKING TYPE LC

DURASTIC ACCODEK OUTSIDE DECKING TYPE LC is a lightweight composition bound with a high solids content natural rubber latex. The surface is finished with a fine grouting material to give a smooth finish. A coat of Durastic Weatherdeck Paint Type AD is applied to give a semi-decorative sealed finish.

WHERE LAID

All external passenger decks but not on the crowns of crew and passenger accommodation where deckhead insulation is not fitted.  May be used on bridge wings, wheelhouse tops, boat decks, games decks, promenade decks etc.  Not to be used on decks of high abuse such as mooring areas, around holds etc., as surface damage may occur.

TECHNICAL DATA

DENSITY:

1,250 kg per m3.

THICKNESS:

5-15 mm per coat.

LAID WEIGHT:

1.25 kg per m² per mm thickness.

COMPRESSIVE STRENGTH:

7 N/mm².

FLEXURAL STRENGTH:

4 point bending test.  Samples 50mm wide 10mm deep 300mm long.  Load applied between 200mm pivots.

Ultimate load 119 Newtons Deflection 2.8mm

Modulus of rupture   4.7 N/mm².

HARDNESS:Indentation 0.2mm after 30 minutes loading of 100kg/cm².

BOND STRENGTH:

Adhesion tested and accepted as being within requirements laid down by the Department of Transport (Marine Directorate) Survey of Crew Accommodation Merchant Ships - Instructions for the Guidance of Surveyors.

THERMAL CONDUCTIVITY:

0.35 W/m K.

SURFACE PREPARATION

STEEL

Steel deck plates must be free from oil, grease, dirt, rust, loose paint etc.

It is essential that all traces of grease and oil are removed before application of the underlay.

A proprietary degreaser should be used.  The steel should be mechanically wire brushed to remove dirt, rust etc., paying particular attention along plate welds and boundary edges.

A mechanical discing machine using 7 inch No. 16 grit (Coarse) discs can be used on heavier deposits.

On older steel in poor condition with a heavier build up of old paint and, perhaps, pitted areas of corrosion it may be necessary to shot blast.

In all cases once the steel has been cleaned and roughened the underlay should be applied as soon as possible before any further rust develops.

ALUMINIUM

Aluminium deck plates must be free from oil, grease, dirt, loose paint etc.

It is essential that all traces of grease and oil are removed before application of the underlay.

A proprietary degreaser should be used.

After degreasing, a coat of Durastic CR60 should be applied and allowed to dry for a minimum of 8 hours, before application of the Durastic underlay.

SHOP PRIMERS

Because of the diversity of shop primers for steel it is impossible to give compatibility information for our underlays with each specific primer in this short section.

However we can say that Durastic Underlays can be applied over a wide range of primers.  In particular the popular rapid curing thin coat two-pack primers are suitable.

Primers containing zinc pigments such as silicates or phosphates usually have tie coats applied to prevent salt formation which makes them suitable.

Normally on a “new build” by the time the deck is released for underlay application the primer is almost walked off.  The installer should have checked that tie-coats had been applied if necessary and then the deck should be prepared by degreasing and removing dirt etc. with a wire brush as detailed in the steel preparation section.

We must stress that if there are any doubts about the type of paint we would much prefer that the installer tell us what primer is on the deck and we will establish with the paint manufacturer the type of paint system before deciding on its compatibility.

COVERAGE

Accodek Main Mix

4 bags   S222 Powder } Covers approx. 9 m²

1 Drum  R42 Liquid     } at a thickness of 10mm

Accodek Grout Coat

2 bags   Grout Powder } Covers approx. 100

1 drum   R42 Liquid     } m² in one coat.

Available in red, green or grey.

Deck Paint

A 5 litre can of Deck Paint Grade A.D. is sufficient to cover an area of approx. 30 m².

Available in red, green or grey

MIXING AND APPLICATION

1)	Clean the deck plates

2)	Lay the Accodek main mix

3)	Apply 1st grout coat

4)	Apply the 2nd grout coat

5)	Apply the paint coat.

Mix together in a metal bath or similar mixing tray, 2 x 25 kilo bag of S222 Powder with approx. 12.5 litres of R42 Liquid.  This should give a fairly stiff mix which is easily trowelled onto deck plates with a plasterer’s type steel trowel.  If the material is soft and sticky to lay, add a little more of the Powder.

The correct consistency is when the material is easy to lay, not sticky and a smooth finish is easily obtained.  The material is applied to the deck plates with a steel trowel to the required thickness (6mm to 10mm) and allowed to dry overnight.  Before applying the first of the two grout coats we recommend that any lumps or trowel marks are removed from the surface of the Accodek main mix, using the edge of a steel trowel or a sanding machine.

The grouting material is made up by using 1 part by volume of R42 Liquid mixed with 2 parts by volume of the grout powder in a clean bucket.  A useful size mix would be composed of 2 litres of R42 Liquid mixed with 4 litres of Grout Powder.  The first coat is applied with a steel trowel held at an angle of approx. 45° and used with a scraping action.  (The thickness of grout coats are approx.  1mm or less per coat).  After the first coat has dried (2-8 hours) a second coat is applied in the same manner as the first coat.  To finish the deck the second coat of grout is allowed to dry and given a coat of Durastic Deck Paint A.D. Grade. If desired a second coat of Durastic Deck Paint A.D.Grade can be applied on the next day.

USEFUL INFORMATION

1)	When laying Accodek Outside Decking in tropical or high temperatures it is important to note the following:-

(a)	Mixing  must  be  carried out in a 	cool, sheltered area.

(b)	The deck upon which  Accodek is 	being laid must be protected from 	the Sun.

2)	One of the most important requirements of deck composition is to ensure that the composition to all boundary edges and around all deck fittings should remain watertight.  A simple method to ensure this is to increase the thickness of the deck compositions at these boundary edges so that water flows away from these danger areas

PACKAGING

S222/           Net:       25.0 kg

Gross:   25.2 kg

Grout           Net        25.0 kg

Gross    25.2 kg

R42              Net       25.0 kg

Gross    26.0 kg

Deck Paint Type AD - 5 litres

STORAGE AND SHELF-LIFE

Accodek powders must be kept in a dry store.  R42 liquid must not be subjected to temperatures below 5°C or above 30°C.  These materials can be stored for a period of 12 months when the above storage conditions prevail.

CERTIFICATES AND APPROVALS

Durastic S222 Underlay (Accodek main coat)  has been tested and approved as a primary underlay fulfilling the requirements of IMO Resolution A.653(16) and A.687(17) and FTP code Annex 1 part 2.

All materials are manufactured and tested using our Quality Management System which has been approved by Lloyds Register Quality Assurance Limited to  ISO 9001 : 2008.

HEALTH AND SAFETY

Normal precautions to avoid inhaling the dust when mixing the powder and to avoid getting the wet product on the skin (as cements are alkaline) should be observed.

Detailed Material Safety Data Sheets and C.O.S.H.H. Assessments are available for safe working with the product.  These should be consulted before commencing work to ensure safe working practice.

TECHNICAL ADVICE

This Data Sheet, although comprehensive, cannot cover every possible application.  Our Technical Department (0191 483 2299) will be pleased to advise on specific applications.

IF IN DOUBT - ASK!