DURASTIC S450 EPOXY UNDERLAY

DURASTIC S450 EPOXY UNDERLAY a filled two part solvent free Epoxy Resin System. It may be used as an underlay to level undulating deck plates before applying decorative or functional epoxy coatings and compositions.

WHERE LAID

On all internal and external decks where a hard, dense, highly chemical, oil and water resistant underlay is required.  An ideal underlay for use in wet spaces, workshops etc., and on weatherdecks.

TECHNICAL DATA

DENSITY:

1,720 Kg per m3.

THICKNESS:

3 - 25 mm in one coat.

LAID WEIGHT:

1.72 Kg per m²  per mm thickness.

COMPRESSIVE STRENGTH:

BS 6319 : Part 2: 1983   33 N/mm².

FLEXURAL STRENGTH:

BS 6319 : Part 3 : 1990  18.7 N/mm².

Displacement at maximum load 2.5mm

BOND STRENGTH:

BS 6319 : Part 4 : 1984 (slant shear method)

18 N/mm².

THERMAL CONDUCTIVITY:

0.30 W/mK.

SURFACE PREPARATION

STEEL

Steel deck plates must be free from oil, grease, dirt, rust, loose paint etc.

It is essential that all traces of grease and oil are removed before application of the underlay.

A proprietary degreaser should be used.  The steel should be mechanically wire brushed to remove dirt, rust etc., paying particular attention along plate welds and boundary edges.

A mechanical discing machine using 7 inch No. 16 grit (Coarse) discs can be used on heavier deposits.

On older steel in poor condition with a heavier build up of old paint and, perhaps, pitted areas of corrosion it may be necessary to shot blast.  In all cases once the steel has been cleaned and roughened the underlay should be applied as soon as possible before any further rust develops.

ALUMINIUM

Aluminium deck plates must be free from oil, grease, dirt, loose paint etc.

It is essential that all traces of grease and oil are removed before application of the underlay.

A proprietary degreaser should be used.

The aluminium should be lightly abraded with a medium grit disc to provide a physical key.

SHOP PRIMERS

Because of the diversity of shop primers for steel it is impossible to give compatibility information for our systems with each specific primer in this short section.

However we can say that Durastic Systems can be applied over a wide range of primers.  In particular the popular rapid curing thin coat two-pack primers are suitable.

Primers containing zinc pigments such as silicates or phosphates usually have tie coats applied to prevent salt formation which makes them suitable.

Normally on a “new build” by the time the deck is released for underlay application the primer is almost walked off.  The installer should have checked that tie-coats had been applied if necessary and then the deck should be prepared by degreasing and removing dirt etc. with a wire brush as detailed in the steel preparation section.

We must stress that if there are any doubts about the type of paint we would much prefer that the installer tell us what primer is on the deck and we will establish with the paint manufacturer the type of paint system before deciding on its compatibility.

COVERAGE

Primer

Coverage depends on the porosity of the substrate but on steel a 4.18 Kg pack of resin/ hardener will cover approximately 10 - 11m².

S450 Epoxy Levelling Coat

- 1 x 3.20 Kg can S450 Resin

- 1 x 0.98 Kg can S450 Hardener

- 1 x 30 Kg S450 Filler

- Covers approx. 3.9m² at 5mm thickness

PROCEDURE

1)	Clean deck plates

2)	Apply S450 Primer

3)	Apply S450 Epoxy levelling coat

4)	Apply Decorative or functional finish.

MIXING AND APPLICATION

Primer

The substrate should be primed with S450 resin / hardener applied sparingly using a roller or brush.

The primer coat is mixed using a stirrer on a drill after adding the hardener to the S450 Resin.

Note/ In smaller areas the main coat can be turned out onto the wet primer and spread into it wet. However on larger jobs it is more practical to prime the deck and then sprinkle in a small amount of S450 filler to form a key and then allow the primer to set before applying the main coat on the next day.

Main Coat

Mix together in a slow speed mixing machine a can of S450 Resin (3.20 Kg) and a can of S450 Hardener 0.98 Kg) for approx. 5 mins.  Gradually add 1 x 30 Kg bag of S450 Filler and mix 3 to 4 minutes or until Filler is mixed thoroughly with the Resin and Hardener.  This is turned out onto the wet primer and laid at approx. 3mm thick or to the required thickness to level the deck using a steel trowel.  This levelling coat is allowed to set overnight.  The next day any small pieces of Epoxy are scraped from the surface and swept clean ready to receive the epoxy decorative or functional coatings.

Ideally the ambient temperature should be 15°C - 25°C when mixing and laying.  It should not be laid below 12°C as curing will be noticeably retarded and the material will be stiffer to use and spread.  The materials should also be stored in warm conditions during the day prior to use.

STORAGE AND SHELF LIFE

Epoxy filler must be kept in a dry store.  Epoxy resin and hardener can be stored in temperatures between 5°C- 35°C.

The materials can be stored for 2 years when the above conditions prevail.

CERTIFICATES AND APPROVALS

Durastic S450 Underlay has been tested and approved as a primary underlay fulfilling the requirements of IMO Resolution A.653(16) and A.687(17) and the International Code for Application of Fire Test Procedures Annex 1 Part 2.

Durastic S450 Underlay complies with the Marine Equipment Directive and has been approved by the leading Marine Approval Societies.  These approvals are updated on an ongoing basis and copies of certificates are available on request.

All materials are manufactured and tested using our Quality Management System which has been approved by Lloyds Register Quality Assurance Limited to 1S0 9001 : 2008.

HEALTH AND SAFETY

Normal precautions to avoid inhaling the dust when mixing the powder and to avoid getting the epoxy resin and hardener onto the skin or eyes should be observed, safety gloves, overalls and goggles should be worn when handling epoxy systems.

Detailed Material Safety Data Sheets and C.O.S.H.H. Assessments are available for safe working with the product.  These should be consulted before commencing work to ensure safe working practice.

TECHNICAL ADVICE

This Data Sheet, although comprehensive, cannot cover every possible application.  Our Technical Department + 44 (0) 191 4832299 will be pleased to advise on specific applications.

IF IN DOUBT - ASK!